## Slide 1: Phases
Component: Pure element or compound: H2O and C12H22O11
Phase: Homogenous portion of material with uniform physical and chemical characteristics - not generally a pure substance, often a liquid solution or solid solution. Example: syrup

## Slide 2: Let’s add sugar to water at 50 C

## Slide 3: Solubility Limits
Solubility limit: Line on a phase diagram separating complete solubility (single phase) and incomplete solubility (two-phase) regions.

## Slide 4: Diagram of Phases
Homogeneous material (solution or single phase)
Heterogeneous material (mixture of two phases)

## Slide 5
Previously we only discussed homogeneous materials (solid solutions / single phase materials)
Example:
Fe-C alloy
Now we discuss, heterogeneous solids / mixtures of solid solutions. We have exceeded the solubility limit and now have more than one phase
A small amount of C was soluble in the Fe lattice.
Only 1 phase.

## Slide 6: Solubility of Cu in Al exceeded
Terms to know:
  Identify the Components vs Phases above
Heterogeneous material (mixture of two phases):
Phases here are “solid solutions”

## Slide 13
Phase Diagrams: Review of Terminology
Terminology:
  Solid Solution
  Mixture
  Solubility Limit
  Component
  Phase
  Solidus
  Liquidus
  Solvus
  Eutectic
  Isomorphous

## Slide 14: Let’s consider a 35wt% Ni – 65wt% Cu alloy at three temperatures: (a) 1300 C, (b) 1250 C, and (c) 1190 C
Identify for each temperature:
Phases Present
Composition of each phase present
Fraction of each phase present

## Slide 15
Consider: Cu-Ni phase diagram
Example of a Binary Isomorphous Phase Diagram
Let’s look at this region

## Slide 16: c10f04
Consider a 35wt% Ni alloy
Components: Cu and Ni.
1. Phases present for 35% Ni at various temperatures:
At 1300°C (a) there is one phase: liquid solution, L.
At 1250°C (c) there are two phases: (1) solid solution a, (2) liquid solution L.
At 1190°C (e) there is one phase: solid solution, a.
 Cu
Ni 
1300°C
1250°C
1190°C

## Slide 17: c10f04
2. Phase compositions
At (a) 100% liquid solution, L
At (c), for the two phases, from the tie line:
(1) L is 32% Ni
(2) a is 43% Ni
At (e) 100% solid solution, a
 Cu
Ni 
Also:
At 1260°C (b) the first solid phase a forms.
At 1220°C (d) the last remaining liquid solidifies.
1220°C
1260°C

## Slide 18: c10f04
At (a) and (b): WL = 1.00
At (d) and (e): Wa = 1.00
At (c), for the two phases,
L (32% Ni) and a (43% Ni):
 Cu
Ni 
3. Mass (weight) fractions
(c)
35
L
32
a
43
%Ni
R
S

## Slide 19
Summary questions on phase diagrams (so far):
At a given temperature and composition, what are the:
  • Phases present?
  • Phase compositions?
  • Weight fractions (mass fraction / phase amounts)?
  • Sketch the microstructure?
For a given composition, for cooling from liquid:
  • At what temperature does the first solid phase form, and what is its composition?
  • At what temperature does the last liquid phase solidify, and what is its composition?