## Slide 1: c11f41
Austenitize
g (FCC) structure
Temper to form
a (BCC) + Fe3C
Martensite, BCT
very hard, brittle
Quenching and
tempering of steels
(one to a few hours)

## Slide 2: c11f34
Tempered
martensite
9300X
Very small
Fe3C particles in
a-Fe matrix
Martensite tempered at ~600°C, which looks like spheroidite except that the Fe3C particles are much smaller.

## Slide 3: c11f35
Mechanical properties of AISI 4340 steel versus tempering
temperature (one-hour temper)

## Slide 4: c11f31
Hardness versus wt% C for plain carbon steels
with various microstructures
Where would martensite and tempered martensite fall on this plot?

## Slide 5: c11f33
Brinell hardness
versus wt% C for
fine pearlite, martensite,
and tempered martensite

## Slide 6: c11f36
Hardness versus tempering time
Times of one or a few hours are usually used.

## Slide 7: c11f20
What happens if we hold just below the eutectoid temperature for a long time?
Example: How would the pearlite structure change? Why?
Does weight fraction of phases change?
Notes: Partially transformed pearlite to spheroidite. Reduce phase boundary area.

## Slide 8: c11f19
Spheroidite
Fe3C phase - in roughly spherical particles, not layers as in pearlite
a-Fe surrounding
the Fe3C particles
What happens if we keep holding this at elevated temperature?
Do weight fractions of phases change?

## Slide 9: c11tf02

## Slide 10: c11f23

## Slide 11: Read about CCT curves
These are straight forward to use.

## Slide 12: c11f26
C-C-T diagram for
eutectoid steel
For constant cooling rates, as in °C/s, a continuous cooling transformation
(C-C-T ) diagram is used.
This is similar to an isothermal T-T-T diagram, but the curves shift some.

## Slide 13: c11f27
C-C-T diagram for
eutectoid steel - cooling rate effect
Two different continuous cooling rates give different results.
“Full Anneal” versus “Normalizing”
Where is Bainite?
Notes: No Bainite. Curve A-B is where Pearlite transformation ceases and we have retained austenite which becomes Martensite.

## Slide 14: c11f28
C-C-T diagram for
eutectoid steel - critical rates
> 140°C/s gives martensite, < 35°C/s gives pearlite, and
intermediate rates give a combination.

## Slide 15: c11f28