## Slide 1
Chapter 4: Imperfections in Solids
In Chap 3, we discussed “perfect” crystalline solids.
In this chapter, we are going to learn about defects that exist in crystalline solids.
Processing can change the number and types of defects in a solid.
Defects often control / alter material properties.

## Slide 2
Chapter 4: Imperfections in Solids
Types of imperfections in crystals
- Point (1D): vacancy, interstitial, substitutional
- Line (2D): dislocations
- Interfacial (3D): surface, grain boundary, twin boundary

## Slide 3: c05f11
Types of imperfections in crystals
point: vacancy, interstitial
line: dislocations
interfacial: grain boundary, twin boundary
Point defects in a metal crystal

## Slide 4
Equilibrium number of vacancies
Vacancies spontaneously form in a solid, with the number
increasing with temperature.
This is an example of the Arrhenius equation, with this general
form applying to a variety of thermally activated processes in
materials science and chemistry.

## Slide 5
Interstitial
impurity
Point defects in a metal or alloy
- the impurity atoms are in solid solution
How big are the interstitial sites in a crystal?
Substitutional
impurity

## Slide 6: Tetrahedral and Octahedral Interstitial Sites in FCC
Use the Crystalline Solids Program to view interstitial sites in the FCC lattice.

## Slide 7: c05f11
Dislocations in a
titanium alloy
at 51,500X
Types of imperfections in crystals
- point: vacancy, interstitial
- line: dislocations
- interfacial: grain boundary, twin boundary

## Slide 8
Notes: John Kacher Dislocation Glide https://youtu.be/EXbiEopDJ_g
Excerpt from a longer film on bubble rafts, possibly made in the 1940s by William Lawrence Bragg. https://youtu.be/P345p7A4IW8

## Slide 9
Notes: John Kacher Dislocation Glide https://youtu.be/EXbiEopDJ_g
Excerpt from a longer film on bubble rafts, possibly made in the 1940s by William Lawrence Bragg. https://youtu.be/P345p7A4IW8

## Slide 10
Notes: John Kacher Dislocation Glide https://youtu.be/EXbiEopDJ_g
Excerpt from a longer film on bubble rafts, possibly made in the 1940s by William Lawrence Bragg. https://youtu.be/P345p7A4IW8

## Slide 11
Notes: John Kacher Dislocation Glide https://youtu.be/EXbiEopDJ_g
Excerpt from a longer film on bubble rafts, possibly made in the 1940s by William Lawrence Bragg. https://youtu.be/P345p7A4IW8

## Slide 12: c05f08
Edge dislocation

## Slide 13: c05f09
Screw dislocation