## Slide 2: Engineering in Al Can
https://youtu.be/hUhisi2FBuw
11 min
Notes: Too long for class but very interesting. Include so students have link.

## Slide 3: c13f01
Classification
of metal alloys
Al, Cu, Mg, Ti,
Co, Ni, etc.
Fe
0.008 - 2.1% C
most < 1% C
< 5% alloys
3 - 4.5% C
1 - 3% Si
most
> 10%
alloys
< 0.25% C
0.25 - 0.6% C
> 0.6% C
> 11% Cr
HSLA
Notes: Note from phase diagram cast irons melt at lower temperatures than steels and are generally cast.

## Slide 4
Cast Iron (> 2.14 wt%)
Typically between 3 and 4.5 wt%
Notes: True equilibrium phase diagram. Cementite is actually metastable and decomposes to alpha-iron and graphite. Slower cooling rates and presence of Silicon (>1 wt%) promotes graphite formation. Cast irons typically have graphite not cementite.

## Slide 5: c14f01
wrought metals
Machining
Chapter 11: Processing of Metals

## Slide 6
Processing Movies:
Forging
Friction Welding
Making of Al Foil
Powder Metallurgy
Investment Casting
How It's Made - Pliers
10 min
5 min
5 min
2 min
2 min
1 min

## Slide 7: c13f01
Recall: Classification
of metal alloys
Al, Cu, Mg, Ti,
Co, Ni, etc.
Fe
0.008 - 2.1% C
most < 1% C
< 5% alloys
3 - 4.5% C
1 - 3% Si
most
> 10%
alloys
< 0.25% C
0.25 - 0.6% C
> 0.6% C
> 11% Cr
HSLA
Let’s look at:
How to measure the affect of processing on mechanical behavior of steel
Precipitation hardening e.g. Al-Cu and Cu-Be

## Slide 8: c11f41
Austenitize
g (FCC) structure
Temper to form
a (BCC) + Fe3C
Martensite, BCT
very hard, brittle
Recall: Quenching and
tempering of steels
(one to a few hours)
(From Ch. 11)

## Slide 11: c14f05
Jominy end-quench bar

## Slide 12: c14f08
Hardness versus Jominy bar position for several steels
These are called
hardenability curves.

## Slide 13: c14f07
Cooling curves for
eutectoid steel
(AISI 1076)

## Slide 14: c14f09
Hardenability curves for AISI 86XX steels
Effect of carbon content

## Slide 15: c14f11
Equivalent Jominy bar distances
- for various locations in bars of different diameters
Water quench
Oil quench

## Slide 16: c14f12
Examples of hardness profiles after quenching
Water quench
Oil quench

## Slide 17: c14f13
Example - Procedure for
estimating hardness profiles
Equivalent distance curves
Hardenability curve
Hardness profile

## Slide 18
This process is used for Al alloys, Ti alloys, Be-Cu alloys, and certain specialty steels.

## Slide 19: c11f41
Precipitation hardening procedure
“Aging” to form
precipitates
Single phase
solid solution
Supersaturated
solution - soft
There is no phase
transformation
in the major alloy.

## Slide 20: c11f41
Precipitation hardening procedure
“Aging” to form
precipitates
Single phase
solid solution
Supersaturated
solution - soft
There is no phase
transformation
in the major alloy.
Note that although this looks similar to the heat treatment procedure for tempered martensite the mechanism is completely different.
Let’s look at the phase diagram for a precipitation hardening alloy to see what is happening.
Notes: Print the hidden slide for student handout.

## Slide 21: c11f40
Schematic phase diagram for precipitation hardening
A-B alloy (C0 wt%) forms a solid solution at T0. Quench to T1, then
heat to T2, where precipitate particles form, and finally cool slowly.
Notes: T0 – Solution heat treatment; T1 – supersaturated alpha phase; T2 – precipitation heat treatment (“aging”)

## Slide 22: c11f40
Schematic phase diagram for precipitation hardening
A-B alloy (C0 wt%) forms a solid solution at T0. Quench to T1, then
heat to T2, where precipitate particles form, and finally cool slowly.
What do you think happens to mechanical properties at T2?
How about as we continue holding at T2?
Notes: T0 – Solution heat treatment; T1 – supersaturated alpha phase; T2 – precipitation heat treatment (“aging”)

## Slide 23: c11f43
Let’s consider a high strength Al alloy: Al-Cu
e.g. AA2024: 4.4% Cu, 1.5% Mg, 0.6% Mn and 93.5% Al

## Slide 24: c11f42
Effect of aging time
Zones = very thin, small disks – 1 to 2 atoms thick, ~ 25 atoms in diam. – not distinct precipitate particles

## Slide 25: c11f42
Effect of aging time
Zones = very thin, small disks – 1 to 2 atoms thick, ~ 25 atoms in diam. – not distinct precipitate particles
Notes: Theta double prime – coherent; theta prime – semicoherent; theta - incoherent

## Slide 26: c11f44
Precipitate particles (schematic)
Supersaturated
solid solution
Coherent particle
Incoherent particle
(overaged)
Very small, evenly dispersed, coherent precipitate particles
have the most benefit.

## Slide 27: c11cof01
Precipitate
particles
Upper wing skin
7150-T651 Al
Al plus wt%
6.2Zn, 2.3Cu,
2.3Mg, 0.12Zr
80,500X TEM
Notes: Note scale here. 100 nm bar!

## Slide 28: c11cof01
Precipitate
particles
Upper wing skin
7150-T651 Al
Al plus wt%
6.2Zn, 2.3Cu,
2.3Mg, 0.12Zr
80,500X TEM
Notes: Note scale here. 100 nm bar!

## Slide 29: c11f45
Effect of aging time
and temperature
2014-T6 Al 4.4Cu, 0.9Si, 0.8Mn, 0.5Mg
syield, MPa
time, h

## Slide 30
Aluminum Strengthening
Illustration by R. W. Landgraf

## Slide 31: c11f51
Cu-Be phase diagram to 4% Be
Non-sparking tools, musical instruments, precision measurement devices, non-magnetic, low temperature applications.
Highest strength of the copper alloys.

## Slide 32
Strengthening of Copper

## Slide 33
Summary: Thermal processing (heat treating) of metals
Annealing - heating, holding at temperature, and then slowly cooling, often to soften the metal.
Process anneal - done to remove the effects of cold work and achieve a fine grain structure.
Stress relief - removal of internal (residual) stresses using a relatively low temperature anneal.
Special annealing processes for steels - normalizing, full annealing, and spheroidizing.
Quenching and tempering - to harden and tailor the properties of steels (Ch. 11).
Precipitation hardening - to harden and tailor the properties of aluminum alloys and other metals (Ch. 11).
Notes: Normalizing – refine grains – austenitize then cool according to CCT
Full Anneal – soften for further processing – austenitize then cool slowly in furnace