## Slide 1
• Grain size reduction
• Solid solution strengthening
• Strain hardening
• Multiple phase effects (Ch. 11)
- quenching and tempering of steels
- precipitation hardening of Al alloys
Because macroscopic plastic deformation corresponds to the motion of large numbers of dislocations, the ability of a metal to plastically deform (yield strength) depends on the relative ease by which dislocations move.

## Slide 2
Principle: Restricting or hindering dislocation motion renders a material harder and stronger.
All strengthening mechanisms rest on this principle.
The question for you to answer is,
“How are dislocations hindered or restricted in any given strengthening mechanism?”

## Slide 3
• Grain size reduction
• Solid solution strengthening
• Strain hardening
• Multiple phase effects (Ch. 11)
- quenching and tempering of steels
- precipitation hardening of Al alloys
Chapter 7: Deformation and Strengthening Mechanisms

## Slide 4: c08f14
Dislocation motion hindered by a grain boundary
At high angle grain boundaries, dislocations tend to “pile up” at grain boundaries. These pile-ups introduce stress concentrations ahead of their slip planes, which generate new dislocations in adjacent grains.
Notes: Because the two grains are of different orientations, a dislocation passing into grain B will have to change its direction of motion; this becomes more diffi- cult as the crystallographic misorientation increases.
The atomic disorder within a grain boundary region will result in a discontinuity of slip planes from one grain into the other.

## Slide 5
Why would a fine grained material have higher strength than a coarse grained material?

## Slide 6
Strengthening by
grain size reduction
Cast Aluminum after inoculation with 25ppm Ti + 5ppm B,
Brass
Notes: Recrystallization results in a finer grain sized material.
Casting with inoculants results in a finer grained material.

## Slide 7: c08f15
Effect of grain size on yield strength (Hall-Petch)
70Cu-30Zn brass

## Slide 8
• Grain size reduction
• Solid solution strengthening
• Strain hardening
• Multiple phase effects (Ch. 11)
- quenching and tempering of steels
- precipitation hardening of Al alloys
Chapter 7: Deformation and Strengthening Mechanisms

## Slide 9: c08f16
Solid solution strengthening
The different size atoms distort
the crystal structure, making the movement of dislocations along their slip planes more difficult.

## Slide 10: c08f04
Distortion and stress local at a dislocation
(Important for understanding strengthening mechanisms.)

## Slide 11: c08f17
Effects of solute atoms
Solute atoms smaller
than host atoms
Solute atoms larger
than host atoms
Compression or
Tension?
Notes: Interactions through the strain fields around dislocation.

## Slide 12
• Grain size reduction
• Solid solution strengthening
• Strain hardening
• Multiple phase effects (Ch. 11)
- quenching and tempering of steels
- precipitation hardening of Al alloys

## Slide 13
Methods of deforming metals
forging
rolling
extruding
drawing
From: Mechanical Behavior of Materials: Engineering Methods for Deformation, Fracture, and Fatigue, 3rd edition, by Norman E. Dowling. ISBN 0-13-186312-6. © 2007 by Pearson Education, Inc., Upper Saddle River, NJ. All rights reserved.

## Slide 14
If applied at room temperature, these procedures are called
cold working and are said to produce strain hardening.
Many new dislocations are
introduced and these interfere
with each other’s motion.

## Slide 15: c08f05
Interactions of
dislocations

## Slide 16: c08f19
Effects of cold work
- strength is increased
What is the tradeoff?

## Slide 17: c08f19
- but ductility is decreased
As for the other methods,
strengthening (good) is
accompanied by reduced
ductility (bad).

## Slide 18: c08f20
Effects of CW on a
low-carbon steel

## Slide 19: A Design Example
made it here lecture 2

## Slide 20: c08f19
Recall: Effects of cold work
- strength is increased
e.g. drawing

## Slide 21
A brass rod with initial diameter d0 = 6.4 mm is to be cold worked by
drawing to achieve syield > 345 MPa and %EL > 20% with final
df = 5.1 mm.
Design Example 7.1, pp. 239
Solution: First consider drawing to d0  df in one step.

## Slide 22: c08f19
%EL
%CW
syield, MPa
syield, ksi
%CW
36.5
410
36.5
8
This gives syield = 410 MPa and %EL = 8%, which is OK for syield
but fails the %EL > 20% requirement.
Goal: achieve syield > 345 MPa and %EL > 20%

## Slide 23: c08f19
%EL
%CW
syield, MPa
syield, ksi
%CW
345
20
20
23
Enter graphs with the required values.
20 to 23% CW is OK; use 21.5% CW as final step.
Goal: achieve syield > 345 MPa and %EL > 20%

## Slide 24
What diameter rod, di , would give our required 21.5% CW?

## Slide 25
Summary:
Draw from 6.4 mm diameter to 5.76 mm (19% CW)
Anneal (recrystallize) to remove CW.
Draw from 5.76 mm diameter to desired 5.1 mm (21.5% CW).
This final step gives about 350 MPa yield strength and 21% EL, exceeding the requirements.

## Slide 26
Lesson 3

## Slide 27
Recovery, recrystallization, and
grain growth

## Slide 28: c08f21ab
Cold-worked brass
- after CW at room temp
- beginning to recrystallize at 580°C

## Slide 29
Why do newly formed crystals appear?
Aren’t we increasing energy by creating more grain boundary area?

## Slide 30: c08f21c-f
- recrystallization proceeds till all of the CW structure is gone at t = 8 s
%CW = 0

## Slide 31: c08f21c-f
Then grain growth begins
- after 15 min at 580°C
- after 10 min at 700°C

## Slide 32: c08f22
Effect of temperature
on structure for 1h
anneal
Annealing - holding a metal
at elevated temperature and
then cooling it slowly, causing
softening or other structural
changes.
The same changes occur with
time at a given temperature.
Time  (at constant temperature)

## Slide 33: c08f24
Grain growth by diffusion

## Slide 34: c08f25
Effect of time and temperature on grain growth

## Slide 35: Extra Slides (not used)

## Slide 36: c08f08
Recall: Macroscopic slip
in a single crystal
- of zinc

## Slide 39: FCC Slip System