## Slide 1
Fracture test – validation of design #just-for-fun
https://youtu.be/Ai2HmvAXcU0
Boeing 777 Wing Test
See Canvas playlist for Chapter 8

## Slide 2
Creep
Creep is deformation that proceeds gradually with time. Such behavior is more prevalent at higher temperatures. In crystalline
materials (metals and ceramics) it becomes significant above 0.3 to 0.6Tm, depending on the material, and it occurs in polymers at room temperature.
Creep rupture occurs when a material gradual tears apart as a result of excessive creep deformation.

## Slide 3: c09f35
Stages of creep
In a creep test at a given temperature, stress is held constant and the increase in strain is measured.

## Slide 4: c09f36
Trends with temperature and stress

## Slide 5: c09f38
Stress vs. creep rate curves
nickel alloy

## Slide 6: c09f37
Stress vs. rupture life curves
nickel alloy

## Slide 7: c09f39
Larsen-Miller plot
Horizontal scale:
PLM = 12,000, 16,000, etc.
From tests done at various stresses s and temperatures T, each giving a rupture time tr , plot s versus PLM, where:
tr in hours, s in MPa,
T in kelvin, K = °C + 273

## Slide 8
A Larsen-Miller parameter plot gives stress as a function of the quantity PLM that combines temperature and rupture time into one variable. Given such a plot, if any two of tr , s, and T are known, the third one can be calculated.
tr in hours, s in MPa, T in Kelvin, K = °C + 273
Rather than reading a graph, it is convenient to fit the data to a
polynomial as follows

## Slide 9
C, log (h) | b0 | b1 | b2 | b3
17 | 38,405 | -8206 | 0 | 0
Example fitted data

## Slide 10
C, log (h) | b0 | b1 | b2 | b3
20 | 116,400 | -120,500 | 53,460 | -8,188
Another example

## Slide 11
C, log (h) | b0 | b1 | b2 | b3
17 | 38,405 | -8206 | 0 | 0
Design Example 9.2
Alloy S-590 is subjected to a stress of 140 MPa at 800°C. Estimate the time to creep rupture.
Solution: Use the data fit just given to calculate the PLM value for the given stress, and from this and the given temperature, calculate the rupture time.

## Slide 13: c09f40
Gas turbine blades
At relatively low stress but high temperature, creep occurs by vacancy diffusion as enhanced by grain boundaries. Hence, larger grain size is beneficial.

## Slide 14
The End