## Slide 1: c10f04
At (a) and (b): WL = 1.00
At (d) and (e): Wa = 1.00
At (c), for the two phases,
L (32% Ni) and a (43% Ni):
 Cu
Ni 
3. Mass (weight) fractions
(c)
35
L
32
a
43
%Ni
R
S

## Slide 2: c10f09
Examples 9.2 and 9.3(a)
11
40
98
For 40 wt% Sn - 60 wt% Pb
at 150°C, find:
Phases present:
(1) a is Pb-rich SS
(2) b is Sn-rich SS
Phase compositions, wt%:
a has 11% Sn, 89% Pb
b has 98% Sn, 2% Pb
Weight (mass) fractions:

## Slide 3: c10f09
Examples 9.2 and 9.3(a)
11
40
98
For 40 wt% Sn - 60 wt% Pb
at 150°C, find:
Weight (mass) fractions:
11
40
98
a
b
0.33
0.67
Phases present:
(1) a is Pb-rich SS
(2) b is Sn-rich SS
Phase compositions, wt%:
a has 11% Sn, 89% Pb
b has 98% Sn, 2% Pb

## Slide 7: Microstructure

## Slide 8: c10f08
Pb-Sn phase diagram – Let’s take a look at microstructure

## Slide 9: c10f11
Pb-Sn - single phase case
For a sufficiently small wt% Sn,
the solubility limit will never be
exceeded, so that a single phase alloy results.
Pb

## Slide 10: c10f12
Pb-Sn - simple
two-phase case
(no eutectic)
For larger wt% Sn, the solubility limit is exceeded on cooling, so that a two-phase material results.
Pb

## Slide 11: c10f13
Pb-Sn eutectic
For 61.9 wt% Sn, a layered eutectic structure is formed.
eutectic point
A
B
A-B is the eutectic line

## Slide 12: c10f14
Pb-Sn eutectic
The dark areas are Pb-rich a solid solution, and the light areas are Sn-rich b solid solution.
375X

## Slide 13: c10f15
Eutectic structure forms only from the liquid phase
82 wt% Pb
98 wt% Sn

## Slide 14
Pb-Sn eutectic
plus primary a
If we drop below 183 C, the L will transform into the eutectic structure, but we already have some a formed in the a + L region above 183 C.

## Slide 15
Pb-Sn eutectic
plus primary a
400X
dark areas = Pb-rich a solid solution
light areas = Sn-rich b solid solution.
a’
Eutectic a
Eutectic b
light
dark
Eutectic structure

## Slide 16: Mass fractions of microconstituents – Eutectic System

## Slide 17
Pb-Sn eutectic
plus primary a
400X
dark areas = Pb-rich a solid solution
light areas = Sn-rich b solid solution.
a’
Eutectic a
Eutectic b
light
dark
Eutectic structure

## Slide 18
Pb-Sn eutectic
plus primary a
If we drop below 183 C, the L will transform into the eutectic structure, but we already have some a formed in the a + L region above 183 C.

## Slide 19
Calculation of fractions of alpha & beta in final microstructure

## Slide 20
See if you can repeat the calculations for a composition greater than 61.9 wt%
Answers:

## Slide 21
The End