## Slide 1: c10f28
Iron - iron carbide (Fe - Fe3C) phase diagram
eutectic pt.
eutectoid pt.
BCC
FCC
BCC

## Slide 2: c10f30
Eutectoid structure
Fe
a + Fe3C eutectoid
- called pearlite
0.76 wt% C
Slowly cool 0.76 wt% C steel from the g region.

## Slide 3: c10f32
Eutectoid formation

## Slide 4: c10f31
Nomenclature
Ferrite: a-iron, BCC structure (magnetic)
Austenite: g-iron, FCC structure (nonmagnetic)
d ferrite: also BCC
Cementite: iron carbide, Fe3C (6.7 wt% C)
Pearlite: a + Fe3C eutectoid (0.76 wt% C)
Iron: < 0.008 wt% C
Steel: 0.008 to 2.1 wt% C, usually < 1%
Cast Iron: ~ 4.5 wt% C

## Slide 5: c10f33
Hypoeutectoid steels
(ferrite-pearlite steels)
0.022 to 0.76 wt% C
Slow cooling from the g region gives a structure of pearlite (eutectoid) plus ferrite (proeutectoid a).
0.76

## Slide 6: c10f34
Ferrite-pearlite steel structure (0.38 wt% C)
635X

## Slide 7: c10f36
0.76
Hypereutectoid steels
(pearlite-cementite steels)
0.76 to 2.14 wt% C
Slow cooling from the g region gives a structure of pearlite (eutectoid) plus cementite (proeutectoid Fe3C).

## Slide 8: c10f37
Pearlite-cementite steel structure (1.4 wt% C)

## Slide 9: c10f34
Calculation of fractions of Proeutectoid Ferrite, Ferrite in Pearlite & Cementite in Pearlite)

## Slide 10
Calculation of fractions of Proeutectoid Ferrite, Ferrite in Pearlite & Cementite in Pearlite)

## Slide 11
Major Concepts
Phase diagram: Graphical representation, for particular components, showing the effect of temperature and composition on the phases present.
Phase transformation: The time dependent process of phase changes when a temperature change crosses a boundary on the phase diagram.
Comment: Phase diagrams as studied in Ch. 9 are equilibrium phase diagrams, as they show the phases after sufficient (sometimes lengthy) time has elapsed for the phase transformations to occur.